Table of references to physical parameters
General remarks
To start with, see the report (TN-2006-00752) for details on the meanings of the various physical parameters and how they are used in the models. In the following table references are given, where available, to the sources of the values of these parameters, for the currently implemented materials.
The inner potential (IP) is not one of the input paramters, but it can be used to estimate the ‘fermi energy’ according to fermienergy = IP – affinity or fermienergy = IP – workfunction, whichever is available.
For anisotropic materials, the longitudinal sound velocity (ul) often differs from the shear one (ut). In this case, the appropriate expression for the sound velocity in this model is us=1/3(2ut + ul) [24, 29]. It has been indicated in the table where this expression has been applied.
Apart from the ‘first’ bandgap, ‘higher’ bandgaps (in particular, direct bandgaps in indirect bandgap semiconductors) have been included as binding energies in the corresponding df files. These higher bandgap energies can be read directly from tables (e.g. in Ref. 19) or deduced from band structure diagrams.

Material	IP	fermienergy	workfunction	affinity	bandgap	soundvelocity	defpotential	lattice	resistivity	remarks
Ag	-	1,2	2	-	-	-	-	-	4
Al	-	1,2	2	-	-	-	-	-	4
Au	-	1,2	2	-	-	-	-	-	4
C (Diamond)	15	-	-	22	28,22	28	19	28,19	-
C (Glassy)	r	-	r	-	r	r	r	r	-	params. set eq. to Graphite
C (Graphite)	3	-	34	-	r	33	33	35	-	treated as a zero-bandgap semiconductor
Cr	-	2	2	-	-	-	-	-	4
Cu	-	1,2,5	2,5	-	-	-	-	-	4
Ge	14	-	-	21	19	19,29t	29	19	-
Fe	-	1,2	2	-	-	-	-	-	4
Ni	-	2	2	-	-	-	-	-	4
Pt	-	2	2	-	-	-	-	-	4
Si	-	2	2	-	21	29,38	29,19	19	-
Sn	-	1	13	-	-	-	-	-	4
Ti	-	1	13	-	-	-	-	-	4	fermi en. calculated
W	-	2	2	-	-	-	-	-	4
Al2O3	-	-	-	11	*	36	12	36	-
AlAs	18	-	-	21	19r	19	20	19	-	direct and indirect
GaAs	17	-	-	21	19	19	26	19	-
GaN	16	-	-	21	19	25t	25	19	-
InAs	17	-	-	21	19	19t	27	19	-
MgO	-	-	-	10,39	10,*	r	r	r	-	fake params. from SiO2
NiSi	-	32r	31	-	-	-	-	-	32	est. from charge carrier dens.
PMMA	-	-	-	r	37	%	%	%	-	source unknown
Polyimide	-	-	-	9r	9r	%	%	%	-	via HOMO and LUMO energy levels
SiC	ra	-	(19)	30	19rb	23,19	19,23	19	-	a. calc. from lattice param. / b. both direct and indirect
Si3N4	-	-	-	8	*	r	r	r	-	fake params. from SiO2
SiO2	-	-	-	6	6	6	6	6	-
TiO2	-	-	-	7	*	%	%	%	-
H2O	-	r	40,r	-	-	%	%	%	-	guessed values

Explanation of symbols
-	Not applicable / not used in the model for this particular material
*	Bandgap estimated from optical data
%	Not available, missing
r	See remarks in the last column
t	The expression us=1/3(2ut + ul) was used for the sound velocity; see above.
()	Reference is given but the parameter is not used for this material.

List of references
1. http://hyperphysics.phy-astr.gsu.edu/hbase/hframe.html, quoting Ashcroft, N. W. and Mermin, N. D., Solid State Physics, Saunders, 1976.
2. Ohya et al., report NIFS-DATA-84, Japan.
3. M.Schowalter et al., Appl.Phys.Lett. 86, 112102 (2005).
4. http://www.webelements.com (also for density, atomic mass values for all elements)
5. Z.-J. Ding and R. Shimizu, Scanning 18, 92-113 (1996).
6. H.-J. Fitting et al., J.Electron Spectrosc.Rel.Phenom. 119, 35-47 (2001).
7. R. Könenkamp, Phys.Rev.B 61, 11057 (2000).
8. G.S. Upadhyaya et al., Appl.Phys.Lett.86, 102101 (2005).
9. E. Itoh and M. Iwamoto, J.Appl.Phys. 81(4), 1790 (1997).
10. D. van Heijnsbergen et al., J.Chem.Phys. 116(6), 2400 (2002).
11. D.V. Morgan et al., J.Phys.D 13, 307 (1980).
12. J. Shan et al., Phys.Rev.Lett. 90(24), 247401 (2003), using model of L.P. Kadanoff, Phys.Rev. 130, 1364 (1963).
13. http://www.environmentalchemistry.com
14. Li et al., Acta Cryst.A 55(4), 652
15. Goswami et al., J.Phys.C 13, 1381 (1980) and references therein
16. Andrew Wong et al., poster presented at the MRS Fall Meeting, Boston, MA, 2005; http://www.rafaldb.com/posters/pics2005/12a.pdf.
17. P. Kruse et al., Ultramicroscopy 96(1), 11 (2003).
18. A. Rosenauer, Electron Holography: AlAs/GaAs Superlattices, pp 193-208 in Transmission Electron Microscopy of Semiconductor Nanostructures, Vol. 182/2003 of Springer Tracts in Modern Physics; and references therein.
19. Several volumes in Landolt-Börnstein, book series, Group III Condensed Matter, Springer-Verlag.
20. Wang et al., PRB 53 (4), 2010
21. http://www.ioffe.rssi.ru/SVA/NSM/Semicond/
22. J.B. Cui et al., Diam.Rel.Mat. 8, 748 (1999).
23. J. Pernot et al., J.Appl.Phys. 90(4), 1869 (2001).
24. C. Jacoboni and L. Reggiani, Rev.Mod.Phys. 55(3), 645 (1983).
25. T. Zubktue and A. Matulionis, Semicond.Sci.Technol. 17, 1144 (2002); and references therein.
26. S.K. Sutradhar and D. Chattopadhyay, J.Phys.C 12, 1693 (1979) and ref. therein.
27. D.L. Rode, Phys.Rev.B 3(10), 3287 (1971). Also contains def. pot values for InSb and InP.
28. L. Reggiani et al., Phys.Rev.B 28(6), 3550 (1983), and refs. therein.
29. S. Smirnov, dissertation at TU Wien, http://www.iue.tuwien.ac.at/phd/smirnov/
30. T.V. Blank et al., Semicond.Sci.Technol. 20, 710 (2005).
31. E. Bucher et al., Appl.Phys.A 40(2), 71 (1986).
32. M. Amiotti et al., Phys.Rev.B 42(14), 8939 (1990).
33. K. Sugihara, Phys.Rev.B 28(4), 2157 (1983).
34. e.g. S. Suzuki et al., J.Electron Spectrosc.Rel.Phenom.114-116, 225 (2001).
35. J.W. McClure, IBM J.Res.Devel.8(3), 255 (1964).
36. http://www.ceramics.nist.gov
37. J.A. Hagen et al., Appl.Phys.Lett.88, 171109 (2006).
38. e.g. M.M. Dignam and A.A. Grinberg, Phys.Rev.B 50(7), 4345 (1994); J.A. Carrillo, to be published in Commun.Comput.Phys. (2007); S.F. Liotta and A. Majorana, arXiv preprint arXiv:cond-mat/0003456v1. None includes a reference to the original data.
39. Ç. Kılıç and A. Zunger, Appl.Phys.Lett. 81(1), 73 (2002).
40. For ice: M.Rapp and F.-J. Lubken, Earth Planets Space 51, 799 (1999).